RUTILE TITANIUM DIOXIDE：BR-767

Production Description:

Inorganic Si, Al surface coating, organic surface treating;

Good whiteness, good optical property and hiding power, good durability etc.

Application:

Universal level, applys to plastic, coating, rubber, masterbatch and paper making etc.

Technical Data:

| Item | Specification |
| --- | --- |
| Purity TiO2 % | ≥ 94 |
| Matter volatile at 105℃ | ≤ 0.8 |
| Hydrotrope % | ≤ 0.5 |
| Residue on sieve 45μm % | ≤ 0.05 |
| Color compare with standard sample | Not lower than |
| Tinting strength compare with standard % | ≥ 112 |
| PH of suspension, aqueous solution retainted | 6.5 ~ 8.5 |
| Oil absorption g/100g | ≤ 22 |
| Resistivity of aqueous extract Ωm | ≥ 50 |
| Matter volatile at 105℃ after 24 hours by(23±2)℃ and relative humidity(50±5) % | ≤ 1 |
| Rutile crystal from conversion % | ≥ 98.5 |
| .μm average particle diameter | 0.22-0.28 |
| Organic matter | YES |
| Packing: 25kg compound paper bags,500kg and 1000kg plastic woven bags as optional. |  |

Qingdao Botian chemical Co., Ltd

Qingdao Tida International Trade Co., Ltd.

Add: 13-101 Hengda Yulan Guoji ,No.702 shanhe Rd.,Chengyang District ,Qingdao ,China

Tel : 86-532-55578891   Mobile phone or whatsapp:0086 13468298184