## Slide 1
Property | SR-2377
Tio2 content | %≥93.0
Rutile content | %≥97.0
Inorganic coating | Zr.Al
Organic treatment | Yes
Solution in water | %≤0.5
Residue | %≤0.01
Whiteness | %≥97.0
L Value | ≥98.0
Tin reducing power | %≥180
Oil absorption,g/100g | 16-20
PH | 6.5-8.5
Specific resistance 2cm | ≥8000
Property | SR-237
Tio2 content | %93.0
Rutile content | %≥97.0
Inorganic coating | Si.Al
Organic treatment | Yes
Loss at 105℃ | %≤0.50
Solution in water | %≤0.5
Residue | %≤0.01
Whiteness | %≥97.0
L Value | ≥98.0
Tint reducing power | %≥180
Oil absorption,g/100g | 17-22
PH | 7.0-9.0
Specific resistance 2 cm | ≥5000
Property | SR-9000
Tio2 content | %≥93.0
Rutile content | %≥97.0
Inorganic coating | Zr.Al
Organic treatment | Yes
Loss at 105℃ | %≤0.50
Solution in water | %≤0.5
Residue | %≤0.01
Whiteness | %≥97.5
L Value | ≥98.0
Tint reducing power | %≥180
Oil absorption,g/100g | 15-18
PH | 6.5-8.5
Specific resistance 2cm | ≥8000
Product Information:
SR-9000 is a rutile Titanium Dioxide powder with silicon and aluminum surface treatment designed for high hiding performance coating and ink applications,the special process design gives SR-9000 titanium dioxide powder high covering,high dispersion and good dispersion stability
Specifications:
Product Information:
SR-237 is a rutile Titanum Dioxide Pigment surface coated by Si and Al inorganic and organic treatment It combines excellent properties such as good whiteness,high durability and good dispersion.
Specifications:
Product Information:
SR-2377 is a rutile Titanium Dioxide Pigment surface coated by Zr and Al inorganic and organic treatment,It designs to give excellent gloss,medium durability and good dispersion.
Specifications:
Applications
Interior/exterior coatings,Industrial paints,Powder coatings,Ink, Furniture paints,Paper,Rubber,Masterbatch,Plastics.
Applications
Carpentry paint,Ink, Automotive paint,Industrial paint, Architectural coating.
青岛钛达和业国际贸易有限公司 Qingdao Tida International Trade Co.,Ltd.
SR-2377
SR-9000
SR- 237
Applications
Water-based coating,Emulsion paint,Powder coating,Paper
青岛渤天化工有限公司 Qingdao Botian Chemical Co.,LTD
Ti達和業